SECTION 07 46 23  WOOD SIDING

PART 1  GENERAL
1.1 SUMMARY
A. Pre-coated architectural wood cladding, soffit and interior lining boards, supplied sealed on all six faces.
1.2 SUBMITTALS
A. Product data for each species, profile and colour specified.
B. Samples of each selected colour, from Crisp Wood Co.
1.3 DELIVERY, STORAGE AND HANDLING
A. Inspect on delivery. Report freight damage at delivery and other concerns to the supplier within 10 days.
B. Store covered, at least 6 in off the ground, with the wrap loosened for airflow.
C. Acclimate to a stable moisture content before installation, confirmed with a moisture meter.
1.4 WARRANTY
A. Crisp Wood Co. 15-year limited warranty, subject to the Crisp maintenance program.

PART 2  PRODUCTS
2.1 MANUFACTURER
A. Basis of design: Crisp Wood Co., Port Coquitlam, BC. 604-254-3325. sales@crispwoodco.com. crispwoodco.com
B. Substitutions: [per Division 01].
2.2 MATERIALS
A. Species and grade: [select one]
1. Western Red Cedar, [Select tight knot (STK)] [Clear mixed grain] [Clear vertical grain], smooth texture.
2. Western Hemlock, clear vertical grain, refined texture. For exterior soffits and interior walls and ceilings only.
3. Lunawood thermally modified Nordic spruce, Select tight knot (STK), smooth texture.
B. Colour: Crisp [colour name].
C. Profile: [1/8 in gap fine line] [S4S] [V-groove, Western Red Cedar only] [Luna Triple tongue and groove, Lunawood only].
D. Size: [nominal size]. Lengths: [lengths].
2.3 COATING
A. Factory-applied premium waterborne multi-coat system, sealed on all six faces.
B. Touch-up: one gallon of matched touch-up supplied with each order.
2.4 ACCESSORIES
A. Fasteners: stainless steel (corrosion-resistant fasteners are required by BCBC 9.27.5.5). Nails to penetrate at least 1.25 in into solid wood.
B. Furring: not less than 1x2 (19 x 38 mm), kiln-dried, straight, free of splits. [Pressure treated where required.]

PART 3  EXECUTION
3.1 INSTALLATION
A. Install to the Crisp Wood Co. Installation Manual. For Lunawood, also follow the Lunawood installation guides; where they differ, the stricter requirement governs.
B. Install over a weather barrier on furring strips to form a drained and vented rainscreen, with an air space not less than 3/8 in (9.5 mm) deep behind the cladding (BCBC 9.27.2.2).
C. Seal all field cuts, cut ends and ripped edges before installation, with the supplied touch-up stain or an alkyd oil end-grain sealer.
D. Clearances: 8 to 12 in above finished ground (BCBC minimum 200 mm) (at least 300 mm for Lunawood), 2 in from the roof, 1 in from adjacent horizontal surfaces.
E. Gaps: 1/8 in at trim, corners and dissimilar materials; 1/4 in at metal; 1/16 in at butt joints.
3.2 MAINTENANCE
A. Wash annually. Re-seal siding, soffits, fascia and trim every five years, and decking every one to three years, with a Crisp-approved sealer.
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